## Slide 1: Data Meeting: Crystallization in Systems of Hard Polyhedra
Richmond S. Newman, Sharon C. Glotzer

## Slide 2: Publications
1. Role of isostaticity and load-bearing microstructure in the elasticity of yielded colloidal gels. Lilian C. Hsiao, Richmond S. Newman, Sharon C. Glotzer, Michael J. Solomon. (2012) PNAS, 109(40), 16029–16034.
  Performed molecular dynamics simulations to help quantify the role of rigid clusters on gel rheology
2. Shape-Driven Colloidal Crystal-Crystal Transitions Xiyu Du, Greg van Anders, Richmond S. Newman, Sharon C. Glotzer. PRL. In review.
  Advised Xiyu on carrying out this project and provided the bulk of the analysis code enabling this research
3. Size- and Shape-Controlled Synthesis of Doped LiYF4 Upconversion Nanophosphors and their Shape-Directed Self-Assembly Xingchen Ye, Joshua E. Collins, Richmond S. Newman, Michael Engel, Jun Chen, Guozhong Xing, Cherie R. Kagan, Sharon C. Glotzer, and Christopher B. Murray. JACS, in preparation.
  Contributed Monte Carlo simulations and provided two mechanisms, truncation or attraction, to explain observed assemblies
4. Shape-Dependent Ordering of Gold Nanocrystals into Large-Scale Superlattices Jianxiao Gong, Richmond S. Newman, Michael Engel, Sharon C. Glotzer, Zhiyong Tang. Nature Nano, submitted.
  Contributed simulations and understanding of the homogeneous and heterogeneous nucleation growth of their gold nanopolyhedra, and understanding of the defects and competing structures inherent to the building blocks
5. Comparing nucleation of rhombic dodecahedra and spheres. Samanthule Nola, Richmond Newman, Julia Dshemuchadse, Sharon C. Glotzer. PRL, in preparation.
  Contributed calculations of thermodynamic driving forces, free energy barriers to nucleation for each shape, and potentials of mean force and torque of each structure, probing how different shapes lead to different crystallization phase behavior.
6. Influence of polyhedral faceting on the crystallization of rotator cubic close packings Richmond Newman, Julia Dshemuchadse, Sharon C. Glotzer. PRL, in preparation.
  Performed calculations showing how a continuous change in shape-parameter effects the nucleation barriers and local fluid and solid structures of a continuously changing family of hard polyhedra.

## Slide 3: Methods: Finding Crystals from Simulation
Cluster particles i if
Wolde, P. Ten, Ruiz-Montero, M., & Frenkel, D. Faraday Discuss. 1996
Notes: “Briefly before we begin I wish to discuss some methods that are important, and that I spent time implementing for our research group to share and reuse” Mention other upgrades of the group analysis code with this, fixing, then eventually reimplementing the periodic boundaries/domain decomposition for performance

## Slide 4: Methods: Rare Events: Umbrella Sampling
Biased Monte Carlo Ensemble
Sample nuclei
sizes
Correct statistics gathered under bias
Compute Free Energy
ten Wolde’s method
Auer, S., & Frenkel, D. J. Chem. Phys. 2004
Notes: Consider explaining this slowly, particularly how the ubias/ and acceptance probabilities are calculated upon a system.

## Slide 5: Paper 1
Role of isostaticity and load-bearing microstructure in the elasticity of yielded colloidal gels. Hsiao, L. C., Newman, R. S., Glotzer, S. C., & Solomon, M. J. (2012) PNAS, 109(40), 16029–16034.
  Performed molecular dynamics simulations to help quantify the role of rigid clusters in gel rheology
  Helped quantify role of contact number and rigidity via simulation using an angular mobility and shape descriptor order parameters

## Slide 6: Paper 2
Shape-Driven Colloidal Crystal-Crystal Transitions Xiyu Du, Greg van Anders, Richmond S. Newman, Sharon C. Glotzer. PRL. In review.
Role in project
  Advised Xiyu on carrying out this project
  Provided a large portion of the analysis code and methods
    Local bond order parameters
    Helped Xiyu implement additional order parameters
    Wrote code for Umbrella Sampling with HOOMD-blue
Project Accomplishments
  First order phase transition discovered between family of face centered cubic and body centered cubic forming polyhedra (right)
  No phase transition between cubes and vertex- truncated cubes from simple cubic to BCC
    Each ‘shape’ adopts a new ‘stable’ crystal structure
  More examples in paper – but shape driven phase transitions may be first order, or not a phase transition at all

## Slide 7: Paper 3
Size- and Shape-Controlled Synthesis of Doped LiYF4 Upconversion Nanophosphors and their Shape-Directed Self-Assembly Xingchen Ye, Joshua E. Collins, Richmond S. Newman, Michael Engel, Jun Chen, Guozhong Xing, Cherie R. Kagan, Sharon C. Glotzer, and Christopher B. Murray. JACS, in preparation.
Project Accomplishments
  Contributed Monte Carlo simulations with a fairly minimal model explaining the experimentally observed structures of parallel and antiparallel striped motifs, body centered tetragonal, and a rolled-parallel phase using a simplified model of the system
  Mapped phase diagrams determining regions describing where each equilibrium structure forms

## Slide 8: Primary goal
Understand driving forces for LiYF4 bipyramids particles on a 2D interface to assemble either parallel or striped phases
100nm
100nm

## Slide 9: Simulation Model
Model as hard polyhedra in Monte Carlo
  Vertices (±1,0,0),(0, ±1,0),(0,0,±A)
Need to confine particles to be quasi-2D
  Apply stiff harmonic spring for vertices outside a narrow window (kz=100, 𝛿z=0.7)

## Slide 10: Example assemblies

## Slide 11
Phase Diagrams

## Slide 12
100nm

## Slide 13
100nm

## Slide 17: Tip truncations
Body centered tetragonal assemblies
Note: 3D structures

## Slide 18: Conclusions: Paper 3
Truncation or short ranged attractions both stabilize the formation of the antiparallel phases
Good parallel phases arise from shorter aspect bipyramids
A second parallel arrangement occurs for heavily truncated bipyramids which roll over
  Mimics behavior of rounded bipyramids in SEMs
Heavily tip truncated bipyramids assemble multi-layer BCT structures instead of monolayers.

## Slide 19: Paper 4
Shape-Dependent Ordering of Gold Nanocrystals into Large-Scale Superlattices. Jianxiao Gong, Richmond S. Newman, Michael Engel, Sharon C. Glotzer, Zhiyong Tang [Nature Nano 2016, submitted]
Project Accomplishments:
  Explained the crystallization processes for of each synthesized gold nanopolyhedra
  Identified and motivated the presence of several octahedron superlattices
  Probed effects of heterogeneous nucleation on the crystal structures and their stability
  Aided in understanding the formation process and quality of the resultant structures

## Slide 20: Large, high quality superlattices

## Slide 21: Millimeter-scale
Same diffraction orientation across sample

## Slide 22: Methods (Experimental)
Gold nanopolyhedra ~30nm edge lengths
Stabilized with CPC (Cetylpyridinium Chloride)
Solvent: Water (mostly)
Particles sediment

## Slide 23: Equilibrium NVT Phase Behavior
Simulations (NVT, Hard particle MC). Equilibrium behavior averaged over 10 replicates of 50e6 MC sweeps. N=2048 particles.
Rhombic dodecahedra and cubes more ‘robust’

## Slide 24: Nucleation

## Slide 25: Typical Homogeneous Growth

## Slide 26: Crystallization timescales

## Slide 27: Identification of octahedra superlattices
Minkowski
Monoclinic
Hexagonal
Notes: Mention the three (Minkowski/trigonal, Monoclinic, and hexagonal). Discuss the relative stability (Hard particle access first two).
Discuss hexagonal structure.

## Slide 28: A solid-solid phase transition

## Slide 29: Heterogeneous Nucleation
Notes: Spheres 51%

## Slide 30: RD: Orientational disorder

## Slide 31: Cubes: Correlated disorder

## Slide 32: Conclusions: Paper 4
Octahedra structure affected by heterogeneous nucleation control and sedimentation favoring Monoclinic packings
Structural Quality
  Rhombic dodecahedra assemble under wide equilibrium conditions but may have orientational defects
  Cubes nucleate easily, but suffer from high vacancy content and local positional disorder
  Octahedra superlattices order well, but with polymorphic equilibrium structures

## Slide 33: Moving onwards
So far we mostly discussed equilibrium hard particle phase behaviors, with some direct measurements of nucleation rates
How does particle shape affect the nucleation processes and thermodynamics of transitioning from fluid to solid?

## Slide 34: Paper 5
Comparing nucleation of rhombic dodecahedra and spheres Samanthule Nola, Richmond Newman, Julia Dshemuchadse, Sharon C. Glotzer. PRL, in preparation.
  Contributed calculations of thermodynamic driving forces, free energy barriers to nucleation for each shape, and potentials of mean force and torque of each structure, probing how different shapes lead to different crystallization phase behavior.
Project Accomplishments
  Compared direct measurements of precritical clusters in the fluid
  Computed chemical potentials for hard rhombic dodecahedra and free energy barriers; find that spheres are significantly harder to nucleate
  Investigate role of shape on the transition from fluid to solid, not merely the equilibrium structure by computing and comparing potentials of mean force and torque in both fluid and solid phases

## Slide 35: Classical Nucleation Theory

## Slide 36: Thermodynamics

## Slide 37: Small particle clusters in the fluid
Pressure?

## Slide 38: Small particle clusters in the fluid
Shown against driving force

## Slide 39: Free Energy Barriers

## Slide 40: Free Energy Maxima

## Slide 41: Potential of Mean Force & Torque

## Slide 42: Potential of Mean Force & Torque

## Slide 43: Conclusions: Paper 5
Shape anistropy allows directional entropic forces between particle pairs to exist in the fluid and these forces manifest at moderate supersaturations
  Cluster size distribution increases faster for RD in fluid
  Nucleation barriers required (at given driving force) is roughly 20kT lower.
    Recall, nucleation rate ~exp(-ΔG/kT).
We suggest the benefit of additional local orientational ordering in the fluid in transitioning to the solid

## Slide 44: Paper 6
Influence of polyhedral faceting on the crystallization of rotator cubic close packings Richmond Newman, Julia Dshemuchadse, Sharon C. Glotzer. PRL, in preparation.
  Performed calculations showing how a continuous change in shape-parameter effects the nucleation barriers and local fluid and solid structures of a continuously changing family of hard polyhedra.
Project Accomplishments
  Demonstrated how a continuous change in shape affects nucleation behaviors in hard particle systems
  Investigated how altered faceting changes local ordering

## Slide 45: Free energy Maxima & Cluster Sizes
Cluster Size
βΔG

## Slide 46: Chemical Potential, Free energies
Free Energy Barrier Height
Free Energy Barrier Height

## Slide 47: Potential Mean Force & Torque
PMFT data for the family (top row liquid, bottom solid).
Truncation undermines local ccp ordering

## Slide 48: Conclusions: Paper 6
We show that the truncation of a rhombic dodecahedra which we knew should weakens the directional entropic forces between pairs of particles leads to higher free energy barriers at a given supersaturation
This provides more evidence that the local structural motifs in the fluid provided by the building block are essential for stabilizing nucleation pathways

## Slide 49: Concluding remarks
Free Energy Barrier Height
Shapes effect both equilibrium assembles and their formation pathways

## Slide 51: Method: Bipyr Local Directional Order
Algorithm:
  For every particle
    Find neighbors (rcut to find adjacent ~4)
    Find bipyr tip with positive z component
    Compute average x-y plane dot product with neighbors
Outcomes:
  Order parameter, -1 is antiparallel, +1 parallel

## Slide 52: Method: Global Axial Order
Algorithm:
  For each particle i
    Calculate xy plane angle theta)
    Calculate c =exp(i*2*theta)
    Calculate phase angle of c, add to list
  Histogram phase angles
    Calculate order parameter as variance of the bin heights
Output:
  Histogram is ~uniform if liquid or many grains
    Variance near zero
  Histogram is sharply peaked if one or few grains
    Variance Large, system has axial alignment

## Slide 53: A diffusionless transformation
In N=4096 systems, the transition reliably (10 replicates, different seeds) undergoes the same transition path
  Say we have a box matrix B1 for the initial Monoclinic lattice with the dense 100 plane perpendicular to the z-axis, and a box B2 after the transition to Minkowski.
  For the larger systems, there exists T s.t. B2 = T B1
    T= [0.9535 -0.0219 0.0618]
    [0.0023 0.9486 -0.0206]
    [0.0979 -0.0670 1.1132]
  T describes how particle positions expand

## Slide 54: PMFT

## Slide 55: PMFT ‘Easy Assembling’ Shapes

## Slide 56
Replace with Custom Slide excising useless subpanels micrographs.
Discuss Oct Separately

## Slide 57: PMFT