## Slide 1: Crystallization in Systems of Hard Polyhedra
Dissertation Defense of Richmond S. Newman
Committee Members: Sharon C. Glotzer, Robert M. Ziff, Michael J. Solomon, and John Kieffer

## Slide 2: Polyhedra Self-Assemble
(above)
P. F. Damasceno, M. Engel, and S. C. Glotzer, “Predictive Self-Assembly of Polyhedra into Complex Structures,” Science (80-. )., vol. 337, no. 6093, pp. 453–457, Jul. 2012.
(left) Jianxiao Gong, Richmond S. Newman, Michael Engel, Sharon C. Glotzer, Zhiyong Tang. “Shape-Dependent Ordering of Gold Nanocrystals into Large-Scale Superlattices,” Nature Comm 2016, submitted

## Slide 3: Material properties and lengthscale
Material properties depend on material length scales
  Colloidal systems can make crystals on scales between 20 nm-1μm.
Ordered metal nanoparticles (Ag, Au) exhibit surface plasmon resonance
  Applications to spectroscopy and catalysis
Light interacts and scatters in crystals with similar wavelengths;
Example: Pollia fruit, shown below contain no blue pigments
Vignolini, S., Rudall, P. J., Rowland, a. V., Reed, A., Moyroud, E., Faden, R. B., … Steiner, U. (2012). Pointillist structural color in Pollia fruit. Proceedings of the National Academy of Sciences, 109(39), 15712–15715. doi:10.1073/pnas.1210105109
Notes: Blue is the pollia fruit, whose color comes from bragg reflection of cellulose microfibrils.

## Slide 4: Why self-assembly?
Numbers required to reach bulk materials:
  An ordered 1 cm3 volume from 100nm cubes requires 1015 particles
Self-assembly can form structures not available to top-down nanoscale fabrication methods, like lithography, film deposition and etching
Haji-Akbari, A., Engel, M., Keys, A. S., Zheng, X., Petschek, R. G., Palffy-Muhoray, P., & Glotzer, S. C. (2009). Disordered, quasicrystalline and crystalline phases of densely packed tetrahedra. Nature, 462(7274), 773–777.

## Slide 5: Overview
Today we will discuss the contributions of simulation to understanding the formation of superlattices in experimental via two case studies:
  Case 1: Self-assembly of bipyramids
  Case 2: Shape-dependent assembly of rhombic dodecahedra, cubes, and octahedra into large-scale superlattices
Following, we discuss simulations of the crystal nucleation process
  Case 3: Faceting, free energy barriers to nucleation, and entropic forces

## Slide 6: Case 1: A Study of Bipyramids
Size- and Shape-Controlled Synthesis of Doped LiYF4 Upconversion Nanophosphors and their Shape-Directed Self-Assembly Xingchen Ye, Joshua E. Collins, Richmond S. Newman, Michael Engel, Jun Chen, Guozhong Xing, Cherie R. Kagan, Sharon C. Glotzer, and Christopher B. Murray. JACS, in preparation.

## Slide 7: Competing Phases
Goal: understand driving forces for LiYF4 bipyramids particles on a 2D interface to assemble either antiparallel or parallel striped phases
100nm
100nm

## Slide 8: Simulation Model
Model as hard polyhedra in Monte Carlo
Need to confine particles to be quasi-2D
  Apply stiff harmonic spring for vertices outside a narrow window (kz=100, 𝛿z=0.7)

## Slide 9: Aspect Ratio

## Slide 10: Aspect Ratio

## Slide 11: Truncations
Local Directional Order measures if particles are locally parallel or antiparallel.

## Slide 12: Non-truncated
100nm

## Slide 13: Moderate truncation
100nm

## Slide 14: Heavy truncation

## Slide 15: Attractive patchy faces

## Slide 16: Tip truncations
Body centered tetragonal assemblies
Note: 3D structures, not planar monolayers

## Slide 17: Bipyramids concluding remarks
Good parallel phases arise from shorter aspect bipyramids
Hard truncation model sufficient to explain the three bipyramid phases via entropy
Interactions between particles also stabilize the novel antiparallel arrangement

## Slide 18: Case 2: Studying Shape, Structure, and Quality
Shape-Dependent Ordering of Gold Nanocrystals into Large-Scale Superlattices. Jianxiao Gong, Richmond S. Newman, Michael Engel, Sharon C. Glotzer, Zhiyong Tang [Nature Comm 2016, submitted]
Project Accomplishments:
  Explained the crystallization processes for of each synthesized gold nanopolyhedra
  Identified and motivated the presence of several octahedron superlattices
  Aided in understanding the formation process and crystal quality of the resultant structures

## Slide 19: Large superlattice assemblies
Gold nanopolyhedra ~40nm edge lengths
Stabilized with cetylpyridinium chloride in water
Particles sediment

## Slide 20: Millimeter-scale
Electron diffractions taken across 0.5mm sample
  Same orientation suggests this is a single domain

## Slide 21: Equilibrium NVT Phase Behavior
Simulations (NVT, Hard particle MC). Equilibrium behavior averaged over 10 replicas.
Rhombic dodecahedra and cubes more ‘robust’ in range of tolerant densities for assembly

## Slide 22: Methods: Finding Crystals from Simulation
Cluster particles i if
Wolde, P. Ten, Ruiz-Montero, M., & Frenkel, D. (1996). Simulation of homogeneous crystal nucleation close to coexistence. Faraday Discuss., 93–110.
Notes: “Briefly before we begin I wish to discuss some methods that are important, and that I spent time implementing for our research group to share and reuse” Mention other upgrades of the group analysis code with this, fixing, then eventually reimplementing the periodic boundaries/domain decomposition for performance

## Slide 23: Nucleation and growth

## Slide 24: Typical Homogeneous Growth
Columns: 20, 50, and 80% crystalline

## Slide 25: Crystallization timescales
Time to nucleate defined by system being 20% crystalline
Growth duration to go from 20-80% crystalline
Diffusion estimates give approximately 104 MC cycles per second
Notes: Add one row of prior slide to this one.

## Slide 26: Octahedra Superlattice Polymorphs
Minkowski
Monoclinic
Hexagonal (2p)
Hexagonal (1p)
Notes: Mention the three (Minkowski/trigonal, Monoclinic, and hexagonal). Discuss the relative stability (Hard particle access first two).
Discuss hexagonal structure.

## Slide 27: Heterogeneous Nucleation
Notes: Spheres 51%

## Slide 28: A solid-solid phase transition
Packing Fraction
Fraction ending as monoclinic
Starts as monoclinic
lattice
Starts as Minkowski
lattice

## Slide 29: RD: Orientational disorder

## Slide 30: Cubes: Correlated disorder
Positional fluctuations and shearing give rise to anisotropic bragg peaks

## Slide 31: Case 2: Concluding remarks
Octahedra structure affected by heterogeneous nucleation control and sedimentation favoring monoclinic packings
Structural Quality
  Rhombic dodecahedra assemble under wide equilibrium conditions but may have orientational defects
  Cubes nucleate easily, but suffer from high vacancy content and local positional disorder
  Octahedra superlattices order well, but with polymorphic equilibrium structures

## Slide 32: Case 3: Crystallization Pathways
New Question: How does particle shape affect nucleation processes and the thermodynamics of transitioning from fluid to solid?
Comparing nucleation of rhombic dodecahedra and spheres Samanthule Nola, Richmond S. Newman, Julia Dshemuchadse, Sharon C. Glotzer. in preparation.
Influence of polyhedral faceting on the crystallization of rotator cubic close packings Richmond S. Newman, Julia Dshemuchadse, Sharon C. Glotzer. in preparation.

## Slide 33: Classical Nucleation Theory

## Slide 34: Tool: Rare Events: Umbrella Sampling
Biased Monte Carlo Ensemble
Sample nuclei
sizes
Correct statistics gathered under bias
Compute Free Energy
Solid-Liquid Order Parameter
Auer, S., & Frenkel, D. (2004). Numerical prediction of absolute crystallization rates in hard-sphere colloids. Journal of Chemical Physics, 120(6), 3015–29.
The point is that we compute nuclei free energies as a function of size
Notes: Consider explaining this slowly, particularly how the ubias/ and acceptance probabilities are calculated upon a system.

## Slide 35: Chemical Potential: Hard Particles
Obligatory Derivation

## Slide 36: Tool: Interfacial Pinning Determines Coexistence Pressure
Abridged instructions: A two-phase system is carefully constructed, and coexistence is determined when conditions are found where there is no tendency to grow or to melt
Pedersen, U. R., Hummel, F., Kresse, G., Kahl, G., & Dellago, C. (2013). Computing Gibbs free energy differences by interface pinning. Physical Review B, 88, 1–5.

## Slide 37: Thermodynamics of the metastable regime

## Slide 38: Free Energy Barriers

## Slide 39: Free Energy Maxima

## Slide 40: Potential of Mean Force & Torque
Expresses local ordering around particles
βF

## Slide 41: Potential of Mean Force & Torque
βF

## Slide 42: Role of Faceting on Nucleation
Study a continuous truncation of rhombic dodecahedra to rhombicuboctahedra that self-assemble face-centered cubic crystals
As the change is continuous we can compare and better understand the role of shape directly

## Slide 43: Thermodynamics

## Slide 44: Free Energy Barrier Heights

## Slide 45: Potentials of Mean Force & Torque
PMFT data for the family (top row liquid, bottom solid).
Truncation undermines local ccp ordering

## Slide 46: Nucleation concluding remarks
Truncations of a rhombic dodecahedra weaken directional entropic forces
Free energy calculations of cluster sizes, and find the truncation causes free energy barriers to rise at given driving forces.
Local structural motifs in the fluid provided by the building block stabilize the nucleation pathways

## Slide 47: Overall concluding remarks
Free Energy Barrier Height
Shapes effect both equilibrium assembles and their formation pathways

## Slide 48: Future Outlook
Nucleation in many polyhedra require local environments to change symmetry
  How will this affect driving forces?
Molecular dynamics of shaped particles allows for faceted particles for direct timescales
DDT
TGR

## Slide 49: Acknowledgements